-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/ep35aolv.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Thermally Conductive Epoxy Features Chemical and High Temperature Resistance

Master Bond EP35AOLV is a two part heat cured epoxy system, designed for bonding, sealing, coating and potting applications. It is a thermally conductive, electrically insulating compound that withstands aggressive chemicals, such as those found in downhole oil and gas processing.  EP35AOLV exhibits superior protection against corrosion in various harsh environments and helps prolong longevity of critical equipment. With a service range that extends from -60°F to 500°F (52°C to 260°C) and a glass transition temperature of around 165-170°C, it is resistant to high temperatures.

The thermal conductivity value for EP35AOLV is 7-8 BTU•in/(ft2 •hr•°F) [1-1.15 W/(m•K)], and its compressive strength measures 24,000-26,000 psi. It is a filled system that has good dimensional stability and low shrinkage upon curing. “EP35AOLV has been designed not only to handle aggressive chemicals, but also to resist high temperature and high pressure environments. Additionally, it has an extremely high tensile modulus of more than 1,000,000 psi at 75°F”, says Rohit Ramnath, Senior Product Engineer.

The ideal cure schedule is 2 to 3 hours at 300°F, followed by 3 to 4 hours at 300-350°F. EP35AOLV has a forgiving 100 to 50 mix ratio by weight, and is flowable, with a mixed viscosity of 50,000-90,000 cps. It adheres well to a wide variety of substrates such as metals, composites, glass, and high temperature plastics such as PEEK. EP35AOLV is available in standard packaging from ounce kits to gallon kits.

Master Bond Chemically Resistant Adhesives

Master Bond EP35AOLV is a two part heat cured epoxy system used for bonding, sealing and encapsulating. It is able to transfer heat and is electrically non-conductive. It withstands aggressive chemicals and high temperatures, such as those found in downhole and other harsh environments. Read more about Master Bond’s chemically resistant adhesives at https://www.masterbond.com/properties/chemical-resistance or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/tds/ep35aolv

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #